## Slide 1
MOF Benchwork: From Benchmark Planning to LAMMPS-Ready Inputs
A reproducible pipeline for MOF adsorption benchmarks
From CRAFTED data to validated LAMMPS input artifacts
MOF Benchwork | Module A preparation

## Slide 2
Project Goal
Build a reproducible benchmark workflow for MOF adsorption simulations.
Focus on Module A first: single-gas CO2 adsorption in MOF-5 / IRMOF-1.
Use CRAFTED data as the source for:
CIF framework structures
force field parameters
adsorbate molecule definitions
reference isotherm data
Start with validated input generation before running full GCMC simulations.
2/18

## Slide 3
Current Architecture
benchmark.py acts as the central pipeline orchestrator.
It does not run simulations directly.
It builds a reproducible run plan from benchmark.json.
Main pipeline steps:
load configuration
normalize defaults
resolve material and force field data
select benchmark module
3/18

## Slide 4
Benchmark Configuration
benchmark.json follows a structured schema:
material
adsorbates
conditions
benchmark
simulation
output
Missing values are filled with sensible defaults.
4/18

## Slide 5
Material and Data Resolution
Implemented MaterialResolver.
Supports aliases such as:
MOF-5
IRMOF-1
Resolves the correct CIF path from CRAFTED.
Charge scheme selection is currently handled during material resolution.
charge_resolver.py is intentionally not implemented yet, because separate charge logic is not needed at this stage.
5/18

## Slide 6
Force Field Resolution
Implemented ForcefieldResolver.
Resolves required UFF files from CRAFTED:
force_field.def
force_field_mixing_rules.def
pseudo_atoms.def
CO2.def
N2.def
Missing adsorbate definitions produce clear errors.
6/18

## Slide 7
CIF to LAMMPS Data Conversion
Implemented converter/cif_to_lammps_data.py.
ASE is used to read geometry and cell vectors.
CIF charges are parsed manually from _atom_site_charge.
This is necessary because ASE does not automatically preserve the CRAFTED charge column.
Output:
framework-only LAMMPS .data
Masses
Atoms # full
7/18

## Slide 8
Restricted Triclinic Box Support
IRMOF-1 is converted into LAMMPS restricted triclinic form.
The converter computes:
lx, ly, lz
xy, xz, yz
Fractional CIF coordinates are transformed into LAMMPS-compatible Cartesian coordinates.
LAMMPS can successfully read the generated structure with read_data.
8/18

## Slide 9
Molecule Template Conversion
Implemented converter/molecule_to_lammps_template.py.
Parses CRAFTED / RASPA molecule definition files.
Currently supports rigid linear molecules such as:
CO2
N2
Generates LAMMPS molecule templates with:
coordinates
atom types
9/18

## Slide 10
Force Field to LAMMPS Conversion
Implemented converter/forcefield_to_lammps.py.
Parses:
pseudo atom masses and charges
Lennard-Jones parameters
Lorentz-Berthelot mixing rule
Builds global atom type assignments:
framework atoms: Zn, H, C, O
CO2 atoms: O_co2, C_co2
10/18

## Slide 11
Unit Conversion and Mixing
CRAFTED stores Lennard-Jones epsilon in Kelvin.
LAMMPS units real expects epsilon in kcal/mol.
Conversion:
CODE: epsilon_kcal_mol = epsilon_K * 0.0019872041
Lorentz-Berthelot mixing:
CODE: sigma_ij = (sigma_i + sigma_j) / 2 | epsilon_ij = sqrt(epsilon_i * epsilon_j)
11/18

## Slide 12
Generated LAMMPS Artifacts
The current workflow can generate:
IRMOF-1.data
framework atoms
framework charges
extra CO2 atom types
bond type capacity for molecule templates
CO2.template
CO2 geometry
12/18

## Slide 13
LAMMPS Smoke Test
A LAMMPS run 0 smoke test was added.
It verifies that LAMMPS can read:
generated .data
generated CO2 molecule template
generated force field include file
Example input:
CODE: units real | atom_style full | boundary p p p | read_data IRMOF-1.data extra/special/per/atom 2 | molecule co2 CO2.template | include forcefield.in | run 0
13/18

## Slide 14
Why extra/special/per/atom 2 Is Needed
The framework .data file initially contains no CO2 molecules.
CO2 is loaded later through a molecule template.
The CO2 template contains bonds.
LAMMPS needs reserved memory for special bonded neighbors.
extra/special/per/atom 2 provides enough capacity for bonded CO2 molecules.
14/18

## Slide 15
Testing Status
Implemented unit and smoke tests in test_benchmark.py.
Current coverage includes:
configuration loading and defaults
material alias resolution
module selection
CRAFTED molecule parsing
CIF charge parsing
restricted triclinic .data generation
15/18

## Slide 16
Development Environment
Conda environment: MOF_sim
Installed and tested:
ASE
LAMMPS
OVITO
LAMMPS version supports:
fix gcmc
fix widom
16/18

## Slide 17
What Has Been Achieved
The project now has a reproducible planning layer.
CRAFTED data can be resolved instead of hard-coded.
IRMOF-1 CIF data can be converted into LAMMPS .data.
CO2 molecule definitions can be converted into LAMMPS molecule templates.
UFF force field parameters can be converted into LAMMPS pair coefficients.
LAMMPS can successfully validate the generated input artifacts with run 0.
17/18

## Slide 18
Next Steps
Add a real --prepare mode to benchmark.py.
Materialize the prepare plan into output directories.
Generate complete Module A LAMMPS input scripts.
Run a very short one-pressure CO2 GCMC test.
Parse basic LAMMPS output.
Only then scale to a full pressure grid and compare against reference isotherms.
18/18